Aisle Containment - RS Doors
GUIDE SPECIFICATIONS
1.0	GENERAL
1.1	SUMMARY
This specification shall define the mechanical characteristics and requirements for the Aisle Containment - RS Doors. 
1.2	STANDARDS
The product shall be designed in accordance with the following agency standards or certifications. Where a conflict arises between these documents and statements made herein, the statements in this specification shall govern.
•	Acrylic Sheet is ASTM D 4802 Category A-2 compliant 
•	Acrylic Panel Specifications:
•	Thickness: 0.236" (6mm)
•	Light Transmittance: 92%
•	Shear Strength: 8.4m psi2 (590 kg/cm 2)
•	Impact Strength: 5 ft.-lb./in.2 (0.35kg/cm2)
•	Maximum Recommended Continuous Temperature: 175°F (79°C)
•	Heat Distortion Temperature: 200°F (93°C)
•	Maximum Shrinkage: 2.5%
•	Water Absorption (Weight Gain on immersion for 24 hours): 0.3%
•	Smoke Density Rating: 13.5%
•	Fuel Contribution Factor: 11,300 BTU/lb.
2.0	PRODUCT
2.1	TYPES
RS Doors may be used with any rack. RS Doors may be used alone or with the Vertical System or the Retractable Roof System. The double sliding doors shall be constructed of black aluminum extrusion, full viewing polycarbonate panels. RS Doors must be anchored to the floor and attached at the top of the rack or in-row equipment. 
•	Aluminum Frame: Black anodized with an ultimate tensile strength of at least 22,000 psi (1517 Bars).
RS Doors	
Cabinet
Height	Actual Height
in. (mm)	Width
in. (mm)	Weight
lb. (kg)	Shipping Weight
lb. (kg)	P/N	
42U	79.33 (2015)	73.3 (1862)	186 (84)	396 (179)	DCAE78DSL	
45U	85.3 (2167)	73.3 (1862)	201 (91)	411 (186)	DCAE84DSL	
48U	90.2 (2291)	73.3 (1862)	207 (94)	418 (190)	DCAE88DSL	
3.0	WARRANTY (U.S. SALES ONLY)
3.1	STANDARD WARRANTY
RS Doors shall be warranted against defects in materials and workmanship for two (2) years from the date of shipment. For the complete warranty terms and description, refer to the separate warranty statement at www.liebert.com.